USE OF RACING TYRES

For most purposes, racing tyres will benefit from an appropriate “scrubbing-in” procedure.  This provides the best combination of performance and longevity under race conditions.

There are several difficulties that arise when using race tyres if they are scrubbed in prior to use.  The most common is “cold graining” where the layer of tread compound in contact with the track, fails in shear with the layer below.  The result is a very visible low frequency, high amplitude rippling effect.  This is more common with new tyres particularly when used in wet, damp or greasy conditions.

Cooper-Avon racing tyres recommend that a standard scrubbing-in procedure be used whenever possible (conditions and regulations permitting).  This consists of subjecting the tyres through one gently heat cycle, gradually loading them up whilst avoiding drifting the car.  This should take about 3/4 laps of the circuit where the lap time is in the region of 60-100 seconds.  The last lap should only be 80% race speed.  If possible, scrub in one new set of tyres during pre-practice, and put these aside for the race.  In this way you will know that they have been balanced correctly, and have no slow punctures, etc.  Getting this done early is important as the qualifying session may become wet or red-flagged, which could forced the use of new tyres in the race.

When regulations or circumstances do not allow the above procedure to be carried out, then the following should be taken into account:-

- Graining of the loading front tyre can be avoided if it is insured that they are fully up to temperature before pushing hard.

- It is relatively easy to generate temperature in the driving tyres as they are transmitting power most of the time.  The front tyres however, will need to be given time and be loaded up progressively before they will be “in” fully.  It should be noted that it is the loading tyres that introduce the significant heat, not sliding or wheel spinning.

- For qualifying, the best results have been shown to have been achieved when the front and rear temperatures are the same when measured at the base of the tread.  If pushed too early, the rear will come in before the front causing under steer and, taken to the extreme, cold graining as detailed above.

- It is quite possible to get the rear tyres to go off before the front tyres come in which will lead to a car that is never balanced, making set up and qualifying very difficult.

Thus, to get the best from a set of scrubbed tyres, look after the rear tyres by not using full power out of corners and instead, work the front tyres progressively without inducing large amounts of under steer.  When the fronts are fully up to temperature, go for a time (really hooked up lap).  Push hard for 2/3 laps, then back off the pace for a lap to allow the tyres to recover and to get some clear track.  Repeat this procedure for best results.

It should be noted that there is always going to be a slight performance peak from new tyres but it will only be possible to take advantage of this if the car is balanced on its tyres.  A correctly scrubbed in set of tyres will always give more consistent performance over its lifetime than a set that has been used hard from new, even if it hasn’t grained.

With thanks to Ron Tauranac